Sulfanor™

Sodium Laureth Sulphate (Type A2, A3, B1, B2, B3)

CAS № 68891-38-3

| Parameter | Value | Test method |
| --- | --- | --- |
|  | Type А2 | Type А3 | Type B1 | Type B2 | Type B3 |  |
| Appearance | colorless or yellowish liquid | thick liquid, colorless or yellowish | Par. 4.2 |
| Active matter, % by weight, not less than | 26-29 | 26-29 | 68-72 | 68-73 | 68-73 | GOST 30828, Par. 3, 4.3 |
| Unsulphonated matter (based on active matter), % by weight, not more than | 3,0 | 4,0 | GOST 30828, Par. 4.6, 4.4 |
| Sodium sulfate, %, not more than | 1,5 | 1,5 | 1,0 | 1,5 | 2,5 | GOST 28478 |
| pH value of 5% water solution, within | 7,5-10 | 7,5-10 | 6,0-8,5 | 7,5-10 | 7,5-13,0 | GOST 22567.5 and Par. 4.5 |
| Diethylene oxide, mg/kg, not more than | 50 | Par. 4.6 |
| Color of 5% water solution, Hazen units, not more than | 30 | 30 | 70 | 30 | 50 | GOST 29131 and Par. 4.7 |

NOTE:

On the costumer’s request it is possible to produce the product of B1, B2, and B3 types with parameter “pH value of 5% water solution” of different value.

PACKAGING:

Polyethylene  barrels 100-250 liters. Tank-containers from stainless steel, heated, capacity 18.6 m3.

APPLICATION:

MPEG is used in production of cosmetics and personal hygiene products, lubricants, adhesives, emulsions, pharmacy, metal works and production of concrete mix additives.

Producer:

Zavod sintanolov LLC

606000, Dzerzhinsk, Nizhny Novgorod region, East industrial area, post box 22

Phone + 7 (831) 272 88 63 / +7 (831) 272 88 59

Fax + 7 (831) 272 88 50

E-mail: mail@norchem.ru

Website: www.norchem.ru